SPECIFICATION Division 07900

CSS(H) Series Foam Seal System

**PART 1 – GENERAL**

**1.01 Summary**

A. The work shall consist of furnishing and installing expansion joints in accordance with the details shown on the plans and the requirements of the specifications. The joints are proprietary designs utilizing polyurethane foam impregnated with a waterproof polymer.

B. Related Work

- Masonry

- Precast concrete

- Cast-in-place concrete

- Curtain Walls

- Metal Cladding

- Sealants and caulking

- Exterior insulation and finish systems

**1.02 Submittals**

A. Template Drawings - Submit typical expansion joint cross-section(s) indicating pertinent dimensioning of opening, profile recess and adjacent construction.

**1.03 Product Delivery, Storage and Handling**

A. Deliver products in each manufacturer's original, intact, labeled containers and store under cover in a dry location until installed. Store off the ground, protect from weather and construction activities.

**1.04 Acceptable Manufacturer**

A. All joints shall be as designed and manufactured by EMS, Inc.,

13311 Main Road, Akron, New York 14001.

B. Alternate manufacturers and their products will be considered, provided they meet the design concept and are produced of materials that are equal to or superior to those called for in the base product specification.

C. Any proposed alternate systems must be submitted and receive approval 21 days prior to the bid. All post bid submittals will not be considered. This submission shall be in accordance with MATERIALS AND SUBSTITUTIONS.

Any manufacturer wishing to submit for prior approval must provide the following:

1. A working 6” sample of the proposed system with a letter describing how system is considered superior to the specified system.

2. A project proposal drawing that illustrates the recommended alternate system installed in the vertical construction that is specific to the project. Typical catalog cut sections will not be considered.

3. Any substitution products not adhering to all specification requirements within will not be considered.

**1.05 Quality Assurance**

A. Manufacturer: Shall have a minimum of ten (10) years of experience specializing in the design and manufacture of expansion joint systems.

**PART 2 - PRODUCT**

**2.01 General**

A. Provide flexible profile manufactured from open-cell polyether urethane foam with a factory applied silicone coating designed to provide protection against moisture and water intrusion on horizontal surfaces. Profile shall be capable of providing a minimum of plus or minus 50% building movement and accommodate moderate variations in width of opening, complex directional change transitions, and resist ultraviolet degradation. The joint areas where this seal applied into for use in the horizontal position, we recommend the additional use of two-part epoxy. In addition to the peal and stick adhesive already placed on the sides of the seal, we supply an epoxy adhesive on the walls of the joint opening.

Provide Pre-Compressed Foam Seal, Model CSS (H) as manufactured by EMS, Inc. and as indicated on drawings for vertical expansion joint locations.

**2.02 Materials**

A. Seal - Profile shall be pre-formed and manufactured from polyurethane impregnated with a waterproof polymer sealing compound that meets ASTM 518, ASTM 283 and DIN 18542. The profile shall meet the requirements of the properties listed in the table below.

**Physical Properties Test Method Results**

Density, lb/ft3 10

Thermal Conductivity 0.05 W/m.°C Temperature Stability Range -40°F to 212°F Tensile Strength ASTM 3574 21 psi Min.

Ultimate Elongation ASTM 3574 ASTM 3574 125% ±20%

Resistance to Compression Set Max 2.5% Shear Strength Min. 8N/cm2

Mildew Resistance Excellent

Staining None

Flammability Self-Extinguishing UL 94VO Meets CAL 117

Self- Extinguishing

Flash Point 590°F (310°C) Durometer Hardness ASTM D2240 Shore A 15 pts.

**2.03 Fabrication**

A. Seal profile shall be shipped in nominal five-foot standard lengths in manufacturer’s standard shipping carton. Seals shall be cut to length on jobsite where required for straight lengths or directional change transitions utilizing appropriate tools, saws and miter boxes. All cuts shall be accurately measured and completed in a neat and workmanlike manner to ensure quality work.

**2.04 Finishes**

A. Seals - Standard color offering: As per Dow Corning 790 Silicone Building Sealant color chart (Precast White, Limestone, Natural Stone, Gray, Black, Bronze, Sandstone, Adobe Tan, Dusty Rose, Rustic Brick, Blue Spruce, Charcoal)

**PART 3 - EXECUTION**

**3.01 Installation**

A. Where indicated and noted on the contract drawings, install seal profiles in a neat workmanlike manner. All surfaces to receive seals shall be free from dirt, water, frost, and any loose foreign debris that may be detrimental to effective joint sealing.

B. Installation contractor shall verify that seal profile is to be installed in the proper width opening for the appropriate temperature at time of installation. Variations in width or incorrect opening that may affect proper installation and product performance shall be brought to the attention of the architect and product manufacturer prior to installation.

C. Install seal profiles in strict accordance with the manufacturer’s typical details and installation procedure in conjunction with the advice of their qualified representative.

**3.02 Clean and Protect**

A. Protect seal profile during construction; after work has been completed in adjacent areas, clean exposed surfaces with a mild cleaner that will not harm or attack the silicone coating.

**END OF SECTION**